Foodgrade Gear Oils

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Flash Point COC, C Min. | Description / Application |
| --- | --- | --- | --- | --- |
| Servosyngear FG 220 Servosyngear FG 320 Servosyngear FG 460 Servosyngear FG 680 | 198 – 242 288 - 352 414 - 506 612 - 748 | 140 144 147 154 | 240 240 240 240 | Servosyngear FG Oils are high performance industrial gear oils specially developed for the lubrication of enclosed gears in food processing machineries. Blended with specially selected synthetic fluids and additives, these products are listed by National Sanitary Foundation (NSF), USA under category H1 for use where there is potential of incidental food contact. |