Synthetic Vacuum Pump Oils

| Product | Kin. Viscosity cSt at 40 C | VI Min. | Pour Point C, Max. | Flash Point COC, C, Min. | Description / Application |
| --- | --- | --- | --- | --- | --- |
| Servovacuum SHC 46 Servovacuum SHC 68 Servovacuum SHC 100 | 42 – 50 62 – 74 90 - 110 | 130 130 140 | (-) 45 (-) 45 (-) 27 | 235 235 220 | Servovacuum SHC oils are fully synthetic vacuum pump oils specially developed for modern industrial applications which require extremely low vacuums. These oils possess low volatility, low pour point, and good anti-wear and frictional characteristics and provide steady vacuum. |