# SERVO 4T

DESCRIPTION

Servo 4T is high performance engine oil for 4 stroke 2/3 wheelers.   This oil is blended from high viscosity index base stocks and contains additives to meet the stated performance standards.

# APPLICATION

Servo 4T is recommended for new generation 4 stroke motorcycles, scooters and auto rickshaws.

# PERFORMANCE STANDARDS

# JASO T903 : API SJ / JASO MA 2

- Meet API SL Specification for Valve Train Wear (VTW)

# SUITABLE FOR :

- M/s Bajaj Auto Ltd.

- M/s TVS Motor Co. Ltd.

- M/s LML Limited.

# PERFORMANCE BENEFITS

- Maximum power output.

- Superior performance in terms of oxidation stability.

- Excellent wear protection at high temperatures and severe operating conditions.

- Outstanding overall engine cleanliness.

- Enhanced engine life.

- Higher fuel efficiency.

- Potential oil drain period of 5000 Kms.

# CHARACTERISTICS

| #### SAE GRADE | ##### 10W-30 | ##### 20W-40 | ##### 20W-50 |
| --- | --- | --- | --- |
| Kin. Viscosity @ 100ºC, cSt | 10– 12 | 13.5 – 15.5 | 16.5 – 17.5 |
| Viscosity Index, Min. | 130 | 110 | 120 |
| ## Flash Point, COC, ºC, Min | 190 | 200 | 200 |
| Pour Point, ºC, Max | (-) 27 | (-) 21 | (-) 21 |
| TBN, mg KOH/gm | 5 – 7 | 5 – 7 | 5 – 7 |
| Sulphated Ash % wt | 0.6 – 0.75 | 0.6 – 0.75 | 0.6 – 0.75 |

Mar-11